
Technical Specifications (to BS EN 771-1)

BRICK MATCH “EAST BARLEY RED BLEND”



Size 65mm

Water Absorption 14%

Compressive Strength 10 N/mm²

Durability F2

Bricks per pack 600

Pack Weight 1.39T

Salt Classification S2

Dimensional Tolerance T2

Dimensional Range R1