Technical Specifications (to BS EN 771-1)

BRICK MATCH “EAST BARLEY RED BLEND”



 Size 65mm

 Water Absorption 14%

 Compressive Strength 10 N/mm²

 Durability F2

 Bricks per pack 600

 Pack Weight 1.39T

 Salt Classification S2

 Dimensional Tolerance T2

 Dimensional Range R1