Document no. 009

APPLICATION: MEDUIM DUTY (TRAFFICKED BY CARS/VANS ONLY & OCCASIONAL DUST CART /TRUCKS up to 31,000kg GVW)

|  | ## AquaGrid 50 |  | AquaGrid 75 |  |
| --- | --- | --- | --- | --- |
| INFILL MATERIAL: | GRASS | GRAVEL | ## GRASS | GRAVEL |
| Depth/type of infill | 40mm of 60:40 sand/soil rootzone | 50mm of 5/14mm gravel to BS 882 | 65mm of 60:40 sand/soil rootzone | 75mm of 5/14mm gravel to BS 882 |
| Bedding Layer | 50mm of 60/40 sand/soil rootzone | 20mm of Zone 2 bedding sand to BS 7533 or 5/14mm gravel to BS 882 | 30mm of 60/40 sand/soil rootzone | 20mm of Zone 2 bedding sand to BS 7533 or 5/14mm gravel to BS 882 |
| Upper Textile (optional) | 200g/m2 non-woven | 200g/m2 non-woven | 200g/m2 non-woven | 200g/m2 non-woven |
| Sub-Base Layer* (assuming CBR of > 5%) | 150mm of specified granular material | 150mm of specified granular material | 150mm of specified granular material | 150mm of specified granular material |
| Lower Textile | 200g/m2 non-woven | 200g/m2 non-woven | 200g/m2 non-woven | 200g/m2 non-woven |
| Geomembrane (if attenuation) | 1.0mm polypropylene | 1.0mm polypropylene | 1.0mm polypropylene | 1.0mm polypropylene |
| Sub-Grade | trimmed & compacted | trimmed & compacted | trimmed & compacted | trimmed & compacted |

### Sub-Base

In accordance with best practice guidance we recommend using an open graded fill.

Ideally a modified MOT Type 1 with fines removed.