PROPOSED RAILINGS AND GATE REFURBISHMENT

AT

5 HAMPSTEAD HILL GARDENS NW3 2PH

METHOD STATEMENT

The existing railings and gate are in poor condition, heavily corroded and unstable.

The existing railings are to be carefully dismantled in sections and removed from site for specialist refurbishment.

Works comprise:

Careful stripping of the black painted finish and removal of all corrosion, scale and contaminants.

Once fully stripped all elements will be subject visual and stress assessment to determine works required to make structurally sound.

Sections beyond repair and will be remade to match original with new matching profiles and castings.

On completion of the refurbishment the railings and gate will have a galvanized layer applied for protection and powder coat finish in gloss black to match the original.

Railings to be re-installed with posts and stanchion ends fully rust-proofed, and set through the stone copings into the top of the wall to match the original construction.